## Slide 1: Microphase Segregation of Polyelectrolyte Brushes
Takashi Yokokura
Advisor: Prof. Rui Wang
UC Berkeley, Chemical and Biomolecular Engineering
Charged and Ion-Containing Polymers I
3/6/2023, 8:00 am - 11:00 am

## Slide 2: Introduction
Polymer brushes are /interesting/ for both applications and biological understanding
Systematic study explores possible phase space for discovery of new conformational targets and possible transition mechanisms

## Slide 3: Motivation
Theory helps to understand mechanisms and structures that are not experimentally available or not predicted
Few theories can handle electrostatics, while others make compromises on polymer physics
Our framework sdflksjd multivalent ions

## Slide 4: System Species and Interactions
(Indices) : Solvent; : Cation; : Anion
Interactions:
Elasticity (monomer-monomer)
Solubility (solvent-monomer)
Electrostatics (ion-monomer)
+
-
+
-
+
-
+
+
+
-
-
-
+
s
s
s
s
s
s
s
s
s
s
s
+
+
+
+
+
+
+
+
+
What is the system made up of?
Polymer curve
Discrete particle locations

## Slide 5: Partition Function Formulation
Elastic entropy following Gaussian statistics
Flory-Huggins short-range interactions
Electrostatic correlations
Local incompressibility
Semicanonical Ensemble
(Indices) : Solvent; : Cation; : Anion
(Subscripts) : Solvent; : Polymer; : Charged
Particle Operators
Coulomb Operator

## Slide 6: Free Energy and SCF Equations
Polymer Density:
Solvent Density:
Incompressibility:
Polymer-controlling Field:
Solvent-controlling Field:
Monomer Probability:
Electrostatic Potential:
Free Energy (ensemble average across surface)
Functional Minimization

## Slide 7: Number of layers tunable with polymer charge fraction
(nm)
High repulsion enriches conformational space
At intermediate repulsion, multiple condensed layers coexist with a dilute layer
High relative attraction eventually causes loss of sensitivity to repulsion
Key observations:
+
+
+
+
+
+
+
+
+
+
Repulsive
Attractive
s
s
s
s
s
s
s
s
s
s
s
s
For (const. repulsive)
Vol. fraction
Smeared charge
Flory-Huggins

## Slide 8: Chain organization within brush is deducible by SCFT
(Endpoint densities x 30)
“Locked-in-layer”
“Pearl-necklace-like”
Two candidates with identical averaged density profiles
4 condensed + 1 dilute
2 condensed
“Locked-in-layer” minimizes elastic penalty using mushroom conformations
Energetic cost of segregation scales with number of monomers within the “stem” traversing layers

## Slide 9: Framework can be used to describe IDP-derived brush
Coarse-graining
Neurofilament Heavy
Experimental Comparison
Beyond Experiments
I
I

## Slide 10: Conclusions
Self-consistent field theory (SCFT) describes coupled interactions and provides ____
High charge fractions broaden the conformational possibilities to microphase segregated brushes
  Mushroom conformations as described in a “locked-in-layer” model
Intrinsically Disordered Protein (IDP) ___

## Slide 11: Acknowledgements
Wang Group
  Prof. Rui Wang
  Dr. Chao Duan
  Nikhil Agrawal
  Luofu Liu
  Dr. Chao Fang
  Ian Woolsey
This material is based upon work supported by the National Science Foundation Graduate Research Fellowship under Grant No. DGE 2146752

## Slide 12: Supplemental Slides