## Slide 1: Vertical Microphase Segregation in Polyelectrolyte Brushes:
Takashi Yokokura
PI: Prof. Rui Wang
September 14th, 10:00 am – 12:00 pm
Qualifying Exam
A Systematic Study and Experimental Validation

## Slide 2: Introduction

## Slide 3: Outline
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC
Experimental Application (Neurofilament-Heavy)
  Cooperative Collapse of the Dilute Layer
Experimental Characterization (Reflectivity)
Future Work
SCFT Build-up
SCF Eqns

## Slide 4: SCFT Build-up — System
Assumptions:
Interactions:
Elasticity (monomer-monomer)
Solubility (solvent-monomer)
Electrostatics (ion-monomer)
+
-
+
-
+
-
+
+
+
-
-
-
+
s
s
s
s
s
s
s
s
s
s
s
+
+
+
+
+
+
+
+
+
Chains within brush identical
Ion correlations neglected
Finite ion volume neglected
What is the system made up of?

## Slide 5: SCFT Build-up — System
Generate fields (equations) that all particles in the system experience
  Continuous functions
  Depend in a mean-field way on all other particles
    “Self-consistent field theory” (SCFT)
+
-
+
-
+
-
+
+
+
-
-
-
+
s
s
s
s
s
s
s
s
s
s
s
+
+
+
+
+
+
+
+
+
111
111
111
What is the end-result of the model?
(Andelman, 2006)

## Slide 6: SCFT Build-up — Interactions
Goal: Adapt framework for free polyelectrolyte in solution to model end-grafted protein brushes in solution
Interactions:
  Elastic entropy following Gaussian statistics
  Flory-Huggins 2-body interactions
  Electrostatics, ignoring any correlations
  Incompressibility

## Slide 7: SCFT Build-up — Partition Function
Semicanonical partition function
  Canonical in polymer, grand canonical in ions and solvent
Particle-to-field transformations
Hubbard-Stratonovich transformation
Saddle-point approximation
Block copolymer formalism

## Slide 8: SCFT Build-up — Free Energy, SCF Eqns
Variational Free Energy
  After statistical average over grafting surface (x-y plane)
Functional Minimization
SCF Equations

## Slide 9: SCFT Build-up — SCF Eqns, cont.
  Mean-field Poisson-Boltzmann Equation
  Modified Diffusion Equation
Block K
Block 2
Block 1

## Slide 10: Outline
Experimental Application (Neurofilament-Heavy)
  Cooperative Collapse of the Dilute Layer
Experimental Characterization (Reflectivity)
Future Work
SCFT Build-up
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC

## Slide 11: Homopolymer,
Grouped by “Conformation”
111
Thresh
Minimum Free Energy Conformations
SCF Eqns

## Slide 12: Solubility = 0.40)

## Slide 13: Solubility at Different Internal Charges

## Slide 14: Internal Structure of xC conformations
2C
(Endpoint densities x 30)
“Locked-in-layer”
“Pearl-necklace-like”
Two candidates with identical averaged density profiles
4Cd

## Slide 15: Outline
Experimental Characterization (Reflectivity)
Future Work
SCFT Build-up
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC
Experimental Application (Neurofilament-Heavy)
  Cooperative Collapse of the Dilute Layer

## Slide 16: Protein Coarse-graining
Coarse-graining performed by grouping charges based on contributions to the slope of the cumulative charge
  Hyperparameters: Number of bins, Minimum number of AA per block
Sample sequence:
  HHHHHHHHHHHHHHH DDDDDDDDDDDDDDDDDDDDDDDDDDDDDD KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK

## Slide 17: Application to NFH, pH 2.4

## Slide 18: Cooperative Collapse of the Dilute Phase
What changes are occurring within NFH during 3x decrease?
Dramatic collapse
Cooperative collapse
2Cd
2C
1C

## Slide 19: Outline
Future Work
SCFT Build-up
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC
Experimental Application (Neurofilament-Heavy)
  Cooperative Collapse of the Dilute Layer
Experimental Characterization (Reflectivity)

## Slide 20: Reflectivity — Method
Validate results by finding layered structures in PEBs
X-ray or neutron reflectivity for characterization of layered films
Specular part of wave momentum transfer vector
Master Equation: Relates density changes to momentum transfer

## Slide 21: Reflectivity — Characteristic Spectra
X-ray and neutron reflectivity
  Direct information on polymer internal structure
  Prior knowledge of possible conformations necessary
(Reinhardt, et. al. Macromolecules, 2013)
Master Equation

## Slide 22: Future Work
xC extension:
  Response to foreign species (e.g. spherical tip of AFM)
  Response to brush-brush
  Multivalent ions (ion correlations)
Experimental Collaborations
  NF(L/M/H) blends for study of biological neurofilaments
    Erika Ding, Prof. Sanjay Kumar
  Nafion aggregation using SCFT-generated force fields and MD
    Siddarth Rajupet, Prof. Clayton Radke

## Slide 23: Summary
xC conformations exist at high internal repulsion
Each chain in xC(d) “locked-in-layer”
NFH dramatic collapse caused by cooperative interactions
Characteristic reflectivity spectra can be generated rigorously

## Slide 24: Acknowledgements

## Slide 25: Summary
Paste from above when finished

## Slide 26: SI: Table of Contents
References
SCFT Build-up
  Flowchart

## Slide 27: References

## Slide 28: SCFT Build-up — Flowchart
PDE Solve (for iteration k)
Propagate (using PDE solutions)
Check (for self-consistency)
Update (if not satisfied)
Anderson Mixing
Simple Mixing
Notation slightly incorrect but changed for clarity. w^{k} = f(w^{k+1/2}, w^{k-1}), where w^{k+1/2} is from SCFT calculations (\phi remains ^{k})

## Slide 29: Reflectivity — Different ’s

## Slide 30: Borisov previous theory
Klushin, Birshtein, Amoskov. (2001). Macromolecules, 34.

## Slide 31: NFH Phase Transition