## Slide 1: Structural and Mechanical Properties of Polyelectrolyte Brushes
Takashi Yokokura
Advisor: Prof. Rui Wang
September 14th, 10:00 am – 12:00 pm
Qualifying Exam

## Slide 2: Introduction
Polymer Brush
  Chains end-fixed to some substrate
  Steric interactions extend chains into solution
Conformational possibilities
  Coexistence between dilute, coil-like layer and condensed layer
Polyelectrolyte Brush
  Monomers contain charge
  Long-range electrostatic interactions drive extension
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
Model system for biological aggregates
  Axon stabilization through neurofilaments
Designable functionalized surface
  Anti-fouling
  “Smart” sensors
Cell-repellant Surface
(Yuan, et. al., J. Cell Sci., 2012)
(Chen, et al., Macromolecules, 2017 )

## Slide 3: Previous Theories
Flory scaling – de Gennes, Alexander
(Xu, et al., Langmuir, 2013)
None can consider multivalent ions
Correlation length:
No. monomers in correlation blob:
Brush height:
Lattice-constrained Scheutjens-Fleer SCFT
(Rubinstein, Colby, Oxford Univ. Press, 2003)
(Yu, et al., Science, 2018)
(Pryamitsyn et al., Macromolecules, 1996)
Our theory:
Captures coupled response of elastic polymer to changing environment
Easily amenable to additional effects/interactions
Minimal approximations

## Slide 4: Outline
Systematic Study (Solubility vs. Internal Charge)
Experimental Characterization (Reflectivity)
Experimental Application (Neurofilament-Heavy)
Future Work
Model and Theory Development
SCF Eqns

## Slide 5: Model and Theory Development — System
Interactions:
Elasticity (monomer-monomer)
Solubility (solvent-monomer)
Electrostatics (ion-monomer)
+
-
+
-
+
-
+
+
+
-
-
-
+
s
s
s
s
s
s
s
s
s
s
s
+
+
+
+
+
+
+
+
+
What is the system made up of?
End-to-end vector
Discrete particle locations

## Slide 6: Model and Theory Development— Interactions
Elastic entropy following Gaussian statistics
Flory-Huggins short-range interactions
Electrostatic correlations over Coulomb operator
Local incompressibility
Semicanonical Ensemble

## Slide 7: Model and Theory Development— Interactions
Particle-to-Field Transformation
111
Saddle-point approximation
Hubbard-Stratonovich Transformation
111

## Slide 8: Model and Theory Development — SCF Eqns
Polymer Density:
Solvent Density:
Incompressibility:
Polymer-controlling Field:
Solvent-controlling Field:
Monomer Probability:
Electrostatic Potential:
Free Energy (ensemble average across surface)
Functional Minimization

## Slide 9: Outline
Experimental Characterization (Reflectivity)
Experimental Application (Neurofilament-Heavy)
Future Work
Model and Theory Development
Systematic Study (VdW Attraction vs. Electrostatic Repulsion)
+
+
+
+
+
+
+
+
+
+
Repulsive
Attractive
s
s
s
s
s
s
s
s
s
s
s
s
Polymer charge fraction
(Electrostatic repulsion)
Hydrophobicity
(VdW attraction)

## Slide 10: Varying VdW () at const. Electrostatic ()
Height
0
0
0
(nm)
Titles, label conformations
Legend?
“phase transition”
“condensed”, not C
Metastable, make first
Phase coex
System:

## Slide 11: Varying VdW () at const. Electrostatic ()
Redundant, maybe first when showing what you’re doing
Different font family for labels (look sharp)
Summary line on every slide
System:

## Slide 12: Solubility at Different Internal Charges
Segmented, fix a020 file, chi attr and alpha repulsion
Observations and key points
* Why they are expected, what do they mean
Don’t say solubility (hydrophobic interactions)
System:

## Slide 13: Internal Structure of xC conformations
(Endpoint densities x 30)
“Locked-in-layer”
“Pearl-necklace-like”
Two candidates with identical averaged density profiles
4Cd
Only one yields correct endpoint distributions
2C
Change
Label solid vs dashed

## Slide 14: Outline
Experimental Application (Neurofilament-Heavy)
  Cooperative Collapse of the Dilute Layer
Future Work
Model and Theory Development
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC
Experimental Characterization (Reflectivity)
Not accurate

## Slide 15: Reflectivity — Method
Validate results by finding layered structures in PEBs
X-ray or neutron reflectivity for characterization of layered films
Specular part of wave scattering vector
Master Equation: Relates density changes to scattering vector
(Schreiber, n.d.)
Merge next slide here

## Slide 16: Reflectivity — Characteristic Spectra
X-ray and neutron reflectivity
  Direct information on polymer internal structure
  Prior knowledge of possible conformations necessary
(Reinhardt, et. al. Macromolecules, 2013)
Master Equation

## Slide 17: Outline
Future Work
Model and Theory Development
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC
Experimental Characterization (Reflectivity)
Experimental Application (Neurofilament-Heavy)
(Srinivasan, 2014)
(Yuan, 2012)
“Heavy”
“… AQGEEEEEAEEGGEEAATTSPPA …”
Not accurate

## Slide 18: Method of Coarse-graining Protein Charge Distribution
Simplifying protein charge distribution is non-trivial
A straight-forward method is to monitor the cumulative sum (cusum)
Sample sequence:
  HHHHHHHHHHHHHHH DDDDDDDDDDDDDDDDDDDDDDDDDDDDDD KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK
incomplete

## Slide 19: Application to NFH, pH 2.4
Merge with previous

## Slide 20: Cooperative Collapse of the Dilute Phase
What changes are occurring within NFH during 3x decrease?
Dramatic collapse
2Cd
2C
1C
“Cooperative collapse”
Too many
Summary line

## Slide 21: Summary
xC conformations exist at high internal repulsion
Each chain in xC(d) “locked-in-layer”
NFH dramatic collapse caused by cooperative interactions
Characteristic reflectivity spectra can be generated rigorously
Feedback from group meeting
SCFT considering…; using that, these phenomena

## Slide 22: Outline
Future Work
SCFT Build-up
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC
Experimental Characterization (Reflectivity)
Experimental Application (Neurofilament-Heavy)
  Cooperative Collapse of the Dilute Layer

## Slide 23: Future Work
xC extension:
  Response to foreign species (e.g. spherical tip of AFM)
  Response to brush-brush
  Multivalent ions (ion correlations)
Experimental Collaborations
  Validation with reflectivity
  NF(L/M/H) blends for study of biological neurofilaments
    Erika Ding, Prof. Sanjay Kumar
  Nafion aggregation using SCFT-generated force fields and MD
    Siddarth Rajupet, Prof. Clayton Radke
Much more specific; physics /interactions of each problem
Highlight difficult problem and not that it’s a collaboration
What is your planned contribution

## Slide 24: Acknowledgements
Prof. Rui Wang
Dr. Chao Duan
Wang Group
Dr. Chao Fang
Nikhil Agrawal
Luofu Liu

## Slide 25: Summary
Paste from above when finished

## Slide 26: SI: Table of Contents
References
Introduction
  Alexander-de Gennes Brush
  SFBox numerical problem
  Borisov, 2001 (1Cd—1C)
SCFT Build-up
  Block copolymer SCFT
  Gaussian Chain
  Particle-to-field Transform,
  Hubbard-Stratonovich Transformation
  Propagator, derivation (CHECK)
  Flowchart (Numerics)
NFH
  Phase transition
  1Cd, 2Cd
Reflectivity
  Various ’s

## Slide 27: References
Abnormal NF image: Yuan, A., Rao, M. V., Veeranna, & Nixon, R. A. (2012). Neurofilaments at a glance. Journal of Cell Science, 125(14), 3257–3263. https://doi.org/10.1242/jcs.104729
Height Profile Figure: Srinivasan, N., Bhagawati, M., Ananthanarayanan, B., & Kumar, S. (2014). Stimuli-sensitive intrinsically disordered protein brushes. Nature Communications, 5(1), 5145. https://doi.org/10.1038/ncomms6145
Alexander-de Gennes Brush: Rubinstein, M., & Colby, R. H. (2003). Polymer Physics, Oxford University Press. New York.
Lubricity Figure: Yu, J., Jackson, N. E., Xu, X., Morgenstern, Y., Kaufman, Y., Ruths, M., de Pablo, J. J., & Tirrell, M. (2018). Multivalent counterions diminish the lubricity of polyelectrolyte brushes. Science, 360(6396), 1434–1438. https://doi.org/10.1126/science.aar5877
XR Multilayer Figure: Xu, H., Penfold, J., Thomas, R. K., Petkov, J. T., Tucker, I., & Webster, J. P. R. (2013). The Formation of Surface Multilayers at the Air–Water Interface from Sodium Polyethylene Glycol Monoalkyl Ether Sulfate/AlCl 3 Solutions: The Role of the Size of the Polyethylene Oxide Group. Langmuir, 29(37), 11656–11666. https://doi.org/10.1021/la4030348
Anti-Biofouling Figure: Chen, W.-L., Cordero, R., Tran, H., & Ober, C. K. (2017). 50th Anniversary Perspective: Polymer Brushes: Novel Surfaces for Future Materials. Macromolecules, 50(11), 4089–4113. https://doi.org/10.1021/acs.macromol.7b00450
XR Layout Figure: Schreiber, F., & Gerlach, A. (n.d.). X-Ray and Neutron Reflectivity. Department of Chemistry - University of Oxford. www.physchem.ox.ac.uk/~fs
XR Spectra Figure: Reinhardt, M., Dzubiella, J., Trapp, M., Gutfreund, P., Kreuzer, M., Gröschel, A. H., Müller, A. H. E., Ballauff, M., & Steitz, R. (2013). Fine-Tuning the Structure of Stimuli-Responsive Polymer Films by Hydrostatic Pressure and Temperature. Macromolecules, 46(16), 6541–6547. https://doi.org/10.1021/ma400962p

## Slide 28: Alexander-de Gennes Brush
Rubinstein, M., & Colby, R. H. (2003). Chapter 5.3
“Correlation length”
Monomers in correlation blobs (self-avoiding walk)
Height = Correlation length x No. Correlation blobs

## Slide 29: Borisov previous theory
Klushin, Birshtein, Amoskov. (2001). Macromolecules, 34.

## Slide 30: SFBox Lattice Artifacts
Pryamitsyn, V. A., Leermakers, F. A. M., Fleer, G. J., & Zhulina, E. B. (1996). Macromolecules, 29(25), 8260–8270.

## Slide 31: Block copolymer Free Energy, SCF Eqns
Variational Free Energy
  After statistical average over grafting surface (x-y plane)
Functional Minimization
SCF Equations

## Slide 32: Block copolymer PDEs
  Mean-field Poisson-Boltzmann Equation
  Modified Diffusion Equation
Block K
Block 2
Block 1

## Slide 33: SCFT Build-up — Flowchart
PDE Solve (for iteration k)
Propagate (using PDE solutions)
Check (for self-consistency)
Update (if not satisfied)
Anderson Mixing
Simple Mixing
Notation slightly incorrect but changed for clarity. w^{k} = f(w^{k+1/2}, w^{k-1}), where w^{k+1/2} is from SCFT calculations (\phi remains ^{k})

## Slide 34: Gaussian Chain
Large N, kb << 1
Generalize to whole chain with free internal segments
Probability of R with N
Bond vector distribution
Local Fluctuation
Configurational integral with free ends

## Slide 35: Particle-to-Field Transform

## Slide 36: Particle-to-Field Transform (2)
Cancels out

## Slide 37: Hubbard-Stratonovich Transformation
Constant, ignored
Electrolyte GCE

## Slide 38: Propagator notation

## Slide 39: Reflectivity — Different ’s

## Slide 40: NFH Phase Transition

## Slide 41: NFH 1Cd, 2Cd