## Slide 1: Structural and Mechanical Properties of Polyelectrolyte Brushes
Takashi Yokokura
Advisor: Prof. Rui Wang
September 14th, 10:00 am – 12:00 pm
Qualifying Exam

## Slide 2: Introduction
Polymer Brush
  Chains end-fixed to some substrate
  Steric interactions extend chains into solution
Conformational possibilities
  Coexistence between dilute, coil-like (vapor) layer and condensed (liquid) layer
Polyelectrolyte Brush
  Monomers contain charge
  Long-range electrostatic interactions drive extension

## Slide 3: Applications
Design and Fundamental Biology
Surface-modification
  Lubrication
  Anti-fouling
  Surface tension
  Stimuli-sensitive (smart) materials
Functionalized aggregation
  Colloid-stabilization
  Protein aggregation (e.g., neurofilaments)
Chen, et al., Macromolecules, 2017 ; Srinivasan, et. al., Nat. Comm., 2014; Yuan, et. al., J. Cell Sci., 2012)
Stimuli-sensitive Brush
Abnormal NF
Cell-repellant Surface
Notes: “Design materials to solve complex problems and understand complex systems which comprise life itself”

## Slide 4: Previous Theories
Flory scaling – de Gennes, Alexander
Rubinstein, Colby, Oxford Univ. Press, 2003; Yu, et al., Science, 2018; Xu, et al., Langmuir, 2013
Field theories
  Standard formulations
  Most common is lattice-constrained
None can consider electrostatic correlations (multivalent ions)
End-points fixed

## Slide 5: Motivations
Effective design requires strong fundamental understanding
Understanding biological systems requires the use of accurate model systems that consider appropriate interactions
We desire a theory to consider complex, coupled interactions between the polymer, the solvent, and other charged species that can
  Provide inaccessible, polymer-level information to experimental data
  Straight-forward incorporation of additional interactions, especially for multivalent systems
Srinivasan, et. al., Nat. Comm., 2014

## Slide 6: Outline
Systematic Study (Solubility vs. Internal Charge)
Experimental Characterization (Reflectivity)
Experimental Application (Neurofilament-Heavy)
Future Work
Model and Theory Development
SCF Eqns

## Slide 7: Model and Theory Development — System
Interactions:
Elasticity (monomer-monomer)
Solubility (solvent-monomer)
Electrostatics (ion-monomer)
+
-
+
-
+
-
+
+
+
-
-
-
+
s
s
s
s
s
s
s
s
s
s
s
+
+
+
+
+
+
+
+
+
What is the system made up of?

## Slide 8: Model and Theory Development — System
Convert from considering discrete particles to continuous, single-particle distributions governed by external fields.
Fields reflect coupled interactions and effect on particle distributions.
  “Self-consistent field theory” (SCFT)
+
-
+
-
+
-
+
+
+
-
-
-
+
s
s
s
s
s
s
s
s
s
s
s
+
+
+
+
+
+
+
+
+
111
111
111
What is the end-result?
p
s
+
−
p

## Slide 9: Model and Theory Development— Interactions
Goal: Adapt framework for free polyelectrolyte in solution to model end-grafted protein brushes in solution
  Elastic entropy following Gaussian statistics
  Flory-Huggins 2-body interactions
  Electrostatics
  Incompressibility
Interactions:

## Slide 10: Model and Theory Development— Partition Function
Semicanonical partition function
  Canonical in polymer, grand canonical in ions and solvent
Particle-to-field transformations
Hubbard-Stratonovich transformation
Saddle-point approximation

## Slide 11: Model and Theory Development— Free Energy
Variational Free Energy
  After statistical average over grafting surface (x-y plane)
Functional Minimization

## Slide 12: Model and Theory Development — SCF Eqns
SCF Equations
(Poisson Boltzmann Equation)
(Modified Diffusion Equation)

## Slide 13: Outline
Experimental Characterization (Reflectivity)
Experimental Application (Neurofilament-Heavy)
Future Work
Model and Theory Development
Systematic Study (Solubility vs. Internal Charge)
+
+
+
+
+
+
+
+
+
+
Repulsive
Attractive
s
s
s
s
s
s
s
s
s
s
s
s

## Slide 14: Solubility sweep,
Grouped by “Conformation”
111
Thresh
Minimum Free Energy Conformations
SCF Eqns

## Slide 15: Solubility sweep, = 0.40, cont.

## Slide 16: Solubility at Different Internal Charges

## Slide 17: Internal Structure of xC conformations
2C
(Endpoint densities x 30)
“Locked-in-layer”
“Pearl-necklace-like”
Two candidates with identical averaged density profiles
4Cd
Only one yields correct endpoint distributions

## Slide 18: Outline
Experimental Application (Neurofilament-Heavy)
  Cooperative Collapse of the Dilute Layer
Future Work
Model and Theory Development
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC
Experimental Characterization (Reflectivity)

## Slide 19: Reflectivity — Method
Validate results by finding layered structures in PEBs
X-ray or neutron reflectivity for characterization of layered films
Specular part of wave scattering vector
Master Equation: Relates density changes to scattering vector
(Schreiber, n.d.)

## Slide 20: Reflectivity — Characteristic Spectra
X-ray and neutron reflectivity
  Direct information on polymer internal structure
  Prior knowledge of possible conformations necessary
(Reinhardt, et. al. Macromolecules, 2013)
Master Equation

## Slide 21: Outline
Future Work
Model and Theory Development
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC
Experimental Characterization (Reflectivity)
Experimental Application (Neurofilament-Heavy)
(Srinivasan, 2014)
(Yuan, 2012)
“Heavy”
“… AQGEEEEEAEEGGEEAATTSPPA …”

## Slide 22: Protein Coarse-graining
Simplifying protein charge distribution is non-trivial
A straight-forward method is to monitor the cumulative sum (cusum)
Sample sequence:
  HHHHHHHHHHHHHHH DDDDDDDDDDDDDDDDDDDDDDDDDDDDDD KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK

## Slide 23: Application to NFH, pH 2.4

## Slide 24: Cooperative Collapse of the Dilute Phase
What changes are occurring within NFH during 3x decrease?
Dramatic collapse
2Cd
2C
1C
“Cooperative collapse”

## Slide 25: Summary
xC conformations exist at high internal repulsion
Each chain in xC(d) “locked-in-layer”
NFH dramatic collapse caused by cooperative interactions
Characteristic reflectivity spectra can be generated rigorously

## Slide 26: Outline
Future Work
SCFT Build-up
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC
Experimental Characterization (Reflectivity)
Experimental Application (Neurofilament-Heavy)
  Cooperative Collapse of the Dilute Layer

## Slide 27: Future Work
xC extension:
  Response to foreign species (e.g. spherical tip of AFM)
  Response to brush-brush
  Multivalent ions (ion correlations)
Experimental Collaborations
  Validation with reflectivity
  NF(L/M/H) blends for study of biological neurofilaments
    Erika Ding, Prof. Sanjay Kumar
  Nafion aggregation using SCFT-generated force fields and MD
    Siddarth Rajupet, Prof. Clayton Radke

## Slide 28: Acknowledgements
Prof. Rui Wang
Dr. Chao Duan
Wang Group
Dr. Chao Fang
Nikhil Agrawal
Luofu Liu

## Slide 29: Summary
Paste from above when finished

## Slide 30: SI: Table of Contents
References
Introduction
  SFBox numerical problem
  Borisov, 2001 (1Cd—1C)
SCFT Build-up
  Block copolymer SCFT
  Flowchart
  Gaussian Chain
  Particle-to-field Transform
  Propagator, derivation
NFH
  Phase transition
  1Cd, 2Cd
Reflectivity
  Various ’s
Theory

## Slide 31: References
Abnormal NF image: Yuan, A., Rao, M. V., Veeranna, & Nixon, R. A. (2012). Neurofilaments at a glance. Journal of Cell Science, 125(14), 3257–3263. https://doi.org/10.1242/jcs.104729
Height Profile Figure: Srinivasan, N., Bhagawati, M., Ananthanarayanan, B., & Kumar, S. (2014). Stimuli-sensitive intrinsically disordered protein brushes. Nature Communications, 5(1), 5145. https://doi.org/10.1038/ncomms6145
Alexander-de Gennes Brush: Rubinstein, M., & Colby, R. H. (2003). Polymer Physics, Oxford University Press. New York.
Lubricity Figure: Yu, J., Jackson, N. E., Xu, X., Morgenstern, Y., Kaufman, Y., Ruths, M., de Pablo, J. J., & Tirrell, M. (2018). Multivalent counterions diminish the lubricity of polyelectrolyte brushes. Science, 360(6396), 1434–1438. https://doi.org/10.1126/science.aar5877
XR Multilayer Figure: Xu, H., Penfold, J., Thomas, R. K., Petkov, J. T., Tucker, I., & Webster, J. P. R. (2013). The Formation of Surface Multilayers at the Air–Water Interface from Sodium Polyethylene Glycol Monoalkyl Ether Sulfate/AlCl 3 Solutions: The Role of the Size of the Polyethylene Oxide Group. Langmuir, 29(37), 11656–11666. https://doi.org/10.1021/la4030348
Anti-Biofouling Figure: Chen, W.-L., Cordero, R., Tran, H., & Ober, C. K. (2017). 50th Anniversary Perspective: Polymer Brushes: Novel Surfaces for Future Materials. Macromolecules, 50(11), 4089–4113. https://doi.org/10.1021/acs.macromol.7b00450
XR Layout Figure: Schreiber, F., & Gerlach, A. (n.d.). X-Ray and Neutron Reflectivity. Department of Chemistry - University of Oxford. www.physchem.ox.ac.uk/~fs
XR Spectra Figure: Reinhardt, M., Dzubiella, J., Trapp, M., Gutfreund, P., Kreuzer, M., Gröschel, A. H., Müller, A. H. E., Ballauff, M., & Steitz, R. (2013). Fine-Tuning the Structure of Stimuli-Responsive Polymer Films by Hydrostatic Pressure and Temperature. Macromolecules, 46(16), 6541–6547. https://doi.org/10.1021/ma400962p

## Slide 32: Borisov previous theory
Klushin, Birshtein, Amoskov. (2001). Macromolecules, 34.

## Slide 33: SFBox Lattice Artifacts
Pryamitsyn, V. A., Leermakers, F. A. M., Fleer, G. J., & Zhulina, E. B. (1996). Macromolecules, 29(25), 8260–8270.

## Slide 34: Block copolymer Free Energy, SCF Eqns
Variational Free Energy
  After statistical average over grafting surface (x-y plane)
Functional Minimization
SCF Equations

## Slide 35: Block copolymer PDEs
  Mean-field Poisson-Boltzmann Equation
  Modified Diffusion Equation
Block K
Block 2
Block 1

## Slide 36: SCFT Build-up — Flowchart
PDE Solve (for iteration k)
Propagate (using PDE solutions)
Check (for self-consistency)
Update (if not satisfied)
Anderson Mixing
Simple Mixing
Notation slightly incorrect but changed for clarity. w^{k} = f(w^{k+1/2}, w^{k-1}), where w^{k+1/2} is from SCFT calculations (\phi remains ^{k})

## Slide 37: Gaussian Chain
Large N, kb << 1
Free internal segments

## Slide 38: Particle-to-Field Transform
Next slide

## Slide 39: Propagator, derivation
Prev slide

## Slide 40: Reflectivity — Different ’s

## Slide 41: NFH Phase Transition

## Slide 42: NFH 1Cd, 2Cd