## Slide 1: Microphase Segregation of Polyelectrolyte Brushes
Takashi Yokokura
Advisor: Prof. Rui Wang
UC Berkeley, Chemical and Biomolecular Engineering
Charged and Ion-Containing Polymers I
3/6/2023, 8:00 am - 11:00 am

## Slide 2: Introduction
Polyelectrolyte brushes (PEBs) are particularly promising for interfacial modification, “smart” materials, and as model systems in biology
A comprehensive understanding of the underlying physics is necessary for
  Discovery of new conformational targets and transition mechanisms
  Polymer design strategies for desired phenomena
(Chen, et al., Macromolecules, 2017 )
Biofouling
pH-sensitive flow valves
Lubrication
(Yuan, et. al., J. Cell Sci., 2012)
Aggregation mechanisms
Protein distribution
Mutation effects

## Slide 3: Motivation
Theory allows for the study of mechanisms and structures throughout the entire parameter space (chain length, charge fraction, solubility, etc.)
Few theories can describe elastic-electrostatic coupling accurately, while others (e.g. lattice-constrained) make compromises on polymer physics
Standard buildup from statistical mechanics allows for straightforward implementation of additional interactions, such as
  Ion fluctuations (multivalent ions / charge inversion)
  Excluded volume effects
  Multi-chain interactions

## Slide 4: System Species and Interactions
(Indices) : Solvent; : Cation; : Anion
Interactions:
Elasticity (monomer-monomer)
Solubility (solvent-monomer)
Electrostatics (ion-monomer)
+
-
+
-
+
-
+
+
+
-
-
-
+
s
s
s
s
s
s
s
s
s
s
s
+
+
+
+
+
+
+
+
+
What is the system made up of?
Polymer curve
Discrete particle locations

## Slide 5: Partition Function Formulation
Elastic entropy following Gaussian statistics
Flory-Huggins short-range interactions
Electrostatic correlations
Local incompressibility
+
-
+
-
+
-
+
+
+
-
-
-
+
s
s
s
s
s
s
s
s
s
s
s
+
+
+
+
+
+
+
+
+

## Slide 6: Free Energy and SCF Equations
Polymer Density:
Solvent Density:
Incompressibility:
Polymer-controlling Field:
Solvent-controlling Field:
Monomer Probability:
Electrostatic Potential:
Free Energy (ensemble average across surface)
Functional Minimization

## Slide 7: Number of layers tunable with polymer charge fraction
High repulsion enriches conformational space
At intermediate repulsion, multiple condensed layers coexist with a dilute layer
High relative attraction eventually causes loss of sensitivity to repulsion
Key observations:
+
+
+
+
+
+
+
+
+
+
Repulsive
Attractive
s
s
s
s
s
s
s
s
s
s
s
s
For (const. repulsive)
Vol. fraction
Smeared charge
Flory-Huggins

## Slide 8: Chain organization within brush is deducible by SCFT
(Endpoint densities x 30)
“Locked-in-layer”
“Pearl-necklace-like”
Two candidates with identical averaged density profiles
4 condensed + 1 dilute
2 condensed
“Locked-in-layer” minimizes elastic penalty using mushroom conformations
Energetic cost of segregation scales with number of monomers within the “stem” traversing layers

## Slide 9: Framework provides structural and mechanistic information for an IDP-derived brush
Coarse-graining
Neurofilament Heavy (NFH)
Experimental Comparison
Beyond Experiments
I
I

## Slide 10: Conclusions
SCFT accurately describes the coupled interactions within PEBs and provides experimentally inaccessible information
High charge fraction facilitates microphase segregation in PEBs
  Each layer as subsequent mushroom conformations (“locked-in-layer” model)
IDP brush derived from NFH is well-described by our model
  Polymer density profiles
  Predicted characterization spectra
    Reflectivity and brush-brush force

## Slide 11: Acknowledgements
Wang Group
  Prof. Rui Wang
  Dr. Chao Duan
  Nikhil Agrawal
  Luofu Liu
  Dr. Chao Fang
  Ian Woolsey
This material is based upon work supported by the National Science Foundation Graduate Research Fellowship under Grant No. DGE 2146752

## Slide 12: Supplemental Slides
Full partition function
NFH pressure dilute-coex transition mechanism

## Slide 13: Full Partition Function
Elastic entropy following Gaussian statistics
Flory-Huggins short-range interactions
Electrostatic correlations
Local incompressibility
Semicanonical Ensemble
(Indices) : Solvent; : Cation; : Anion
(Subscripts) : Solvent; : Polymer; : Charged
Particle Operators
Coulomb Operator

## Slide 14: NFH pressure dilute-coex transition
Original figure
4 mM vs. 6 mM mechanisms