## Slide 1: a040x170s020

## Slide 2: a040x170s010

## Slide 3: Micelle / Stripe / Cylinder
s = 5e-03, N = 50, a = 0.0, x = 1.0
s = 5e-03, N = 75, a = 0.0, x = 1.0
Isosurface at pha = 0.1
s = 5e-03, N = 105, a = 0.05, x = 1.0
s = 5e-03, N = 140 a = 0.10, x = 1.0

## Slide 4: a040x170s025

## Slide 5: a040x170s022

## Slide 6: a040x170 seed
cyl4-12
cyl4-975
cyl16-1025
cyl16-975
cyl1
See if becomes hex

## Slide 7: a040x170s017

## Slide 8: a040x170s015 seed
Almost done
Almost done

## Slide 9: a040x170s013

## Slide 10: a040x170s010 seed

## Slide 11: X200 x170 x130 x120 x100
F = −10.24458
F = − 9.14301
F = −9.63949
F = − 9.63030
F = −11.0015
F = −10.9948
F = −11.0057
F = −10.9953
F = −10.2429
F = −10.2461
F = −10.2431

## Slide 12: a040x100 relaxation

## Slide 13: a040x100 seed
old
old

## Slide 14: a040x120 relaxation
F = −10.24458

## Slide 15: a040x120 seed
cyl16-850
cyl16-825

## Slide 16: a040x130 relaxation

## Slide 17: a040x170 relaxation
F = −9.10347
1 neck

## Slide 18: a040x200 relaxation

## Slide 19: a040x200 seed
Note: not completely converged but stopped for resources

## Slide 20: a0.40 x1.70

## Slide 21: Zhulina JCP 1998
Zhulina NVT; current GCE runs at Lz = 20
0.1 mM
1 mM
10 mM
25 mM
a = 0.01
May need to init using sine

## Slide 22: Carrillo Langmuir 2009

## Slide 23: Parallelization

## Slide 24: Equations
Quenched average, np, A --> \inf ; np/A  \sigma
Discrete Gaussian chain

## Slide 25: Scaling (Alexander—de Gennes brush)
V = 4.2; H = 27.5 – 30.5
V = 2; H = 39 – 45.5

## Slide 26: : DGC (3D; NxNy=1) vs MDE (1D)
Ns/sigs: dz = 0.10, Ngz_2 = 4; Chis/bs: dz = 0.25, Ngz_2 = 3.5

## Slide 27: Numericals
Ys
Possibly do Ngz for multiple dzs

## Slide 28: 3D
Lxy = 1
Lxy = 5
y-z heatmaps for at constant x
Lxy = 10
Lxy = 15

## Slide 29: z-FFT vs z-FD (MDE) – REDFT01 xy(z)
Lx = 5, Ly = 5, Lz = 50. s = 0.02. x = 0.75. a = 0.00, N = 50
3D vs 1D (dashed): dz = 0.5, ds = 0.20; dz_1D = 0.113, ds_1D = 0.083
FFT (yz vs pha)
FD (yz vs pha)
FD (xyz)
FFT (xyz)
Diff btw 1D/3D should just be dz, ds, etc.

## Slide 30: Specifying Grafted Points

## Slide 31: Strategy
2D binary array for surface sites of homogeneously grafted polymer given grafting density, simulation box size, and discretization (and assuming dx = dy)
Fullspace must be periodic on x0 = xL, y0 = yL
Halfspace must be even on xL/2 and yL/2 (overlap of boundary following REDFT00) and periodic on x0 = xL, y0 = yL.
Homogeneous spacing as determined by regular hexagon, where grafting point at centroid of hexagon
In case there are edge effects, try shifting the centroids away from the boundaries of the xy-plane (only did for fullspace)
Make sure no edge effects by comparing results of full FFT with cos FFT

## Slide 32: Test conditions
Sigma = 0.05 c/nm2
Lx = 15 nm
Ly = 15 nm
dx = 0.4 nm
Cast in terms of dx (for rounding and PBC for grafting points):
Sigma = 0.0668 c/nm2
Lx = 14.80 nm
Ly = 11.20 nm
(Sigma error decrease with dx)

## Slide 33
Padded PBC (Full FFT)
Hexagons drawn for illustration of hexagon approach

## Slide 34
Unpadded PBC (Full/Cos FFT)

## Slide 35: Other conditions (full and half results overlapped to show match)
s = 0.0241 (20.28%; dx=0.4), Lx, Ly = 12.40, 20.80
s = 0.0208 (4.08%; dx=0.1), Lx, Ly = 12.90, 22.30
s = 0.1332 (11%; dx=0.1), Lx, Ly = 20.50, 20.40