## Slide 1: Vertical Microphase Segregation in Polyelectrolyte Brushes:
Takashi Yokokura
PI: Prof. Rui Wang
September 14th, 10:00 am – 12:00 pm
Qualifying Exam
A Systematic Study and Experimental Validation

## Slide 2: Introduction
Polymer Brush
  Chains end-fixed to some substrate
  Steric interactions extend chains into solution
Abnormal NF (Yuan, 2012)
Applications
  Biofouling
  “Smart” (stimuli-sensitive) materials
  Underlying physics of protein systems (neurofilament)
Conformational possibilities
  Coexistence between dilute, coil-like (vapor) layer and condensed (liquid) layer
Polyelectrolyte Brush
  Monomers contain charge
  Long-range electrostatic interactions drive extension
(Srinivasan, 2014)

## Slide 3: Outline
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC
Experimental Application (Neurofilament-Heavy)
  Cooperative Collapse of the Dilute Layer
Experimental Characterization (Reflectivity)
Future Work
SCFT Build-up
SCF Eqns

## Slide 4: SCFT Build-up — System
Assumptions:
Interactions:
Elasticity (monomer-monomer)
Solubility (solvent-monomer)
Electrostatics (ion-monomer)
+
-
+
-
+
-
+
+
+
-
-
-
+
s
s
s
s
s
s
s
s
s
s
s
+
+
+
+
+
+
+
+
+
Chains within brush identical
Ion correlations neglected
Finite ion volume neglected
What is the system made up of?

## Slide 5: SCFT Build-up — System
Generate fields (equations) that all particles in the system experience
  Continuous functions
  Depend in a mean-field way on all other particles
    “Self-consistent field theory” (SCFT)
+
-
+
-
+
-
+
+
+
-
-
-
+
s
s
s
s
s
s
s
s
s
s
s
+
+
+
+
+
+
+
+
+
111
111
111
What is the end-result of the model?
(Andelman, 2006)

## Slide 6: SCFT Build-up — Interactions
Goal: Adapt framework for free polyelectrolyte in solution to model end-grafted protein brushes in solution
  Elastic entropy following Gaussian statistics
  Flory-Huggins 2-body interactions
  Electrostatics
  Incompressibility
Interactions:

## Slide 7: SCFT Build-up — Partition Function
Semicanonical partition function
  Canonical in polymer, grand canonical in ions and solvent
Particle-to-field transformations
Hubbard-Stratonovich transformation
Saddle-point approximation
Block copolymer formalism

## Slide 8: SCFT Build-up — Free Energy, SCF Eqns
Variational Free Energy
  After statistical average over grafting surface (x-y plane)
Functional Minimization
SCF Equations

## Slide 9: SCFT Build-up — SCF Eqns, cont.
  Mean-field Poisson-Boltzmann Equation
  Modified Diffusion Equation
Block K
Block 2
Block 1

## Slide 10: Outline
Experimental Application (Neurofilament-Heavy)
  Cooperative Collapse of the Dilute Layer
Experimental Characterization (Reflectivity)
Future Work
SCFT Build-up
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC

## Slide 11: Solubility sweep,
Grouped by “Conformation”
111
Thresh
Minimum Free Energy Conformations
SCF Eqns

## Slide 12: Solubility sweep, = 0.40, cont.

## Slide 13: Solubility at Different Internal Charges

## Slide 14: Internal Structure of xC conformations
2C
(Endpoint densities x 30)
“Locked-in-layer”
“Pearl-necklace-like”
Two candidates with identical averaged density profiles
4Cd

## Slide 15: Outline
Experimental Characterization (Reflectivity)
Future Work
SCFT Build-up
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC
Experimental Application (Neurofilament-Heavy)
  Cooperative Collapse of the Dilute Layer

## Slide 16: Protein Coarse-graining
Simplifying protein charge distribution is non-trivial
A straight-forward method is to monitor the cumulative sum (cusum)
Sample sequence:
  HHHHHHHHHHHHHHH DDDDDDDDDDDDDDDDDDDDDDDDDDDDDD KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK

## Slide 17: Application to NFH, pH 2.4

## Slide 18: Cooperative Collapse of the Dilute Phase
What changes are occurring within NFH during 3x decrease?
Dramatic collapse
2Cd
2C
1C
“Cooperative collapse”

## Slide 19: Outline
Future Work
SCFT Build-up
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC
Experimental Application (Neurofilament-Heavy)
  Cooperative Collapse of the Dilute Layer
Experimental Characterization (Reflectivity)

## Slide 20: Reflectivity — Method
Validate results by finding layered structures in PEBs
X-ray or neutron reflectivity for characterization of layered films
Specular part of wave scattering vector
Master Equation: Relates density changes to momentum transfer

## Slide 21: Reflectivity — Characteristic Spectra
X-ray and neutron reflectivity
  Direct information on polymer internal structure
  Prior knowledge of possible conformations necessary
(Reinhardt, et. al. Macromolecules, 2013)
Master Equation

## Slide 22: Outline
Future Work
SCFT Build-up
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC
Experimental Application (Neurofilament-Heavy)
  Cooperative Collapse of the Dilute Layer
Experimental Characterization (Reflectivity)

## Slide 23: Future Work
xC extension:
  Response to foreign species (e.g. spherical tip of AFM)
  Response to brush-brush
  Multivalent ions (ion correlations)
Experimental Collaborations
  Validation with reflectivity
  NF(L/M/H) blends for study of biological neurofilaments
    Erika Ding, Prof. Sanjay Kumar
  Nafion aggregation using SCFT-generated force fields and MD
    Siddarth Rajupet, Prof. Clayton Radke

## Slide 24: Summary
xC conformations exist at high internal repulsion
Each chain in xC(d) “locked-in-layer”
NFH dramatic collapse caused by cooperative interactions
Characteristic reflectivity spectra can be generated rigorously

## Slide 25: Acknowledgements
Prof. Rui Wang
Dr. Chao Duan
Wang Group
Dr. Chao Fang
Nikhil Agrawal
Luofu Liu

## Slide 26: Summary
Paste from above when finished

## Slide 27: SI: Table of Contents
References
SCFT Build-up
  Flowchart
  Gaussian Chain
  Particle-to-field Transform
NFH
  Phase transition
  1Cd, 2Cd
Reflectivity
  Various ’s
Theory
  Borisov, 2001 (1Cd—1C)

## Slide 28: References
Abnormal NF image: Yuan, A., Rao, M. V., Veeranna, & Nixon, R. A. (2012). Neurofilaments at a glance. Journal of Cell Science, 125(14), 3257–3263. https://doi.org/10.1242/jcs.104729
Andelman, D. (2006). Introduction to electrostatics in soft and biological matter. In W.C.K. Poon, D. Andelman (Eds.), Soft Condensed Matter Physics in Molecular and Cell Biology (pp. ). CRC Press.
Srinivasan, N., Bhagawati, M., Ananthanarayanan, B., & Kumar, S. (2014). Stimuli-sensitive intrinsically disordered protein brushes. Nature Communications, 5(1), 5145. https://doi.org/10.1038/ncomms6145
Schreiber, F., & Gerlach, A. (n.d.). X-Ray and Neutron Reflectivity. Department of Chemistry - University of Oxford. www.physchem.ox.ac.uk/~fs
Reinhardt, M., Dzubiella, J., Trapp, M., Gutfreund, P., Kreuzer, M., Gröschel, A. H., Müller, A. H. E., Ballauff, M., & Steitz, R. (2013). Fine-Tuning the Structure of Stimuli-Responsive Polymer Films by Hydrostatic Pressure and Temperature. Macromolecules, 46(16), 6541–6547. https://doi.org/10.1021/ma400962p

## Slide 29: SCFT Build-up — Flowchart
PDE Solve (for iteration k)
Propagate (using PDE solutions)
Check (for self-consistency)
Update (if not satisfied)
Anderson Mixing
Simple Mixing
Notation slightly incorrect but changed for clarity. w^{k} = f(w^{k+1/2}, w^{k-1}), where w^{k+1/2} is from SCFT calculations (\phi remains ^{k})

## Slide 30: Gaussian Chain
Large N, kb << 1
Free internal segments

## Slide 31: Particle-to-Field Transform

## Slide 32: Reflectivity — Different ’s

## Slide 33: Borisov previous theory
Klushin, Birshtein, Amoskov. (2001). Macromolecules, 34.

## Slide 34: NFH Phase Transition

## Slide 35: NFH 1Cd, 2Cd