## Slide 1: Structural and Mechanical Properties of Polyelectrolyte Brushes
Takashi Yokokura
Advisor: Prof. Rui Wang
September 14th, 10:00 am – 12:00 pm
Qualifying Exam

## Slide 2: Introduction
Polymer Brush
  Chains end-fixed to some substrate
  Steric interactions extend chains into solution
Conformational possibilities
  Coexistence between dilute, coil-like layer and condensed layer
Polyelectrolyte Brush
  Monomers contain charge
  Long-range electrostatic interactions drive extension
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
Model system for biological aggregates
  Axon stabilization through neurofilaments
Designable functionalized surface
  Anti-fouling
  “Smart” sensors
Cell-repellant Surface
(Yuan, et. al., J. Cell Sci., 2012)
(Chen, et al., Macromolecules, 2017 )

## Slide 3: Previous Theories
Flory scaling – de Gennes, Alexander
(Xu, et al., Langmuir, 2013)
None can consider multivalent ions
Correlation length:
No. monomers in correlation blob:
Brush height:
Lattice-constrained Scheutjens-Fleer SCFT
(Rubinstein, Colby, Oxford Univ. Press, 2003)
(Yu, et al., Science, 2018)
(Pryamitsyn et al., Macromolecules, 1996)
Our theory:
Captures coupled response of elastic polymer to changing environment
Easily amenable to additional effects/interactions
Minimal approximations

## Slide 4: Outline
Systematic Study (Solubility vs. Internal Charge)
Experimental Characterization (Reflectivity)
Experimental Application (Neurofilament-Heavy)
Future Work
Model and Theory Development
SCF Eqns

## Slide 5: Model and Theory Development — System
Interactions:
Elasticity (monomer-monomer)
Solubility (solvent-monomer)
Electrostatics (ion-monomer)
+
-
+
-
+
-
+
+
+
-
-
-
+
s
s
s
s
s
s
s
s
s
s
s
+
+
+
+
+
+
+
+
+
What is the system made up of?
End-to-end vector
Discrete particle locations

## Slide 6: Model and Theory Development— Interactions
Elastic entropy following Gaussian statistics
Flory-Huggins short-range interactions
Electrostatic correlations over Coulomb operator
Local incompressibility
Semicanonical Ensemble

## Slide 7: Model and Theory Development— Interactions
Particle-to-Field Transformation
111
Saddle-point approximation
Hubbard-Stratonovich Transformation
111

## Slide 8: Model and Theory Development — SCF Eqns
Polymer Density:
Solvent Density:
Incompressibility:
Polymer-controlling Field:
Solvent-controlling Field:
Monomer Probability:
Electrostatic Potential:
Free Energy (ensemble average across surface)
Functional Minimization

## Slide 9: Outline
Experimental Characterization (Reflectivity)
Experimental Application (Neurofilament-Heavy)
Future Work
Model and Theory Development
Systematic Study (VdW Attraction vs. Electrostatic Repulsion)
+
+
+
+
+
+
+
+
+
+
Repulsive
Attractive
s
s
s
s
s
s
s
s
s
s
s
s
Polymer charge fraction
(Electrostatic repulsion)
Hydrophobicity
(VdW attraction)

## Slide 10: Varying VdW () at const. Electrostatic ()
Height
0
0
0
(nm)
System:
C = “condensed” layer(s)
Polymer distribution
Polymer smeared charge
Flory-Huggins parameter
Free energy
Brush microphase segregates to locally balance repulsive and attractive forces

## Slide 11: Varying VdW and Smeared Charge Fraction
System:
Polymer distribution
Polymer smeared charge
Flory-Huggins parameter
Higher polymer charge leads to richer conformational space
Coexistence with dilute layer adjacent to the dilute regime
As attraction becomes dominant, brushes will be identical
Attraction
Repulsion

## Slide 12: Chain Architecture of Multi-peaked Conformations
(Endpoint densities x 30)
“Locked-in-layer”
“Pearl-necklace-like”
Two candidates with identical averaged density profiles
4 condensed + 1 dilute
Chains stay within one layer, regardless if condensed or dilute
2 condensed

## Slide 13: Outline
Experimental Application (Neurofilament-Heavy)
  Cooperative Collapse of the Dilute Layer
Future Work
Model and Theory Development
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC
Reflectivity Spectra for the Validation of Multi-peak conformations

## Slide 14: Reflectivity — Method
Validate results by finding layered structures in PEBs
X-ray or neutron reflectivity for characterization of layered films
Specular part of wave scattering vector
Master Equation: Relates density changes to scattering vector
(Schreiber, n.d.)
Merge next slide here

## Slide 15: Reflectivity — Characteristic Spectra
X-ray and neutron reflectivity
  Direct information on polymer internal structure
  Prior knowledge of possible conformations necessary
(Reinhardt, et. al. Macromolecules, 2013)
Master Equation

## Slide 16: Outline
Future Work
Model and Theory Development
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC
Experimental Characterization (Reflectivity)
Experimental Application (Neurofilament-Heavy)
(Srinivasan, 2014)
(Yuan, 2012)
“Heavy”
“… AQGEEEEEAEEGGEEAATTSPPA …”
Not accurate

## Slide 17: Method of Coarse-graining Protein Charge Distribution
Simplifying protein charge distribution is non-trivial
A straight-forward method is to monitor the cumulative sum (cusum)
Sample sequence:
  HHHHHHHHHHHHHHH DDDDDDDDDDDDDDDDDDDDDDDDDDDDDD KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK
incomplete

## Slide 18: Application to NFH, pH 2.4
Merge with previous

## Slide 19: Cooperative Collapse of the Dilute Phase
What changes are occurring within NFH during 3x decrease?
Dramatic collapse
2Cd
2C
1C
“Cooperative collapse”
Too many
Summary line

## Slide 20: Summary
Multi-peaked conformations form to locally balance competing interactions.
These conformations are exclusive to polyelectrolyte brushes.
Each chain is allowed in only one layer. Outer layers are “grafted” upon inner layers.
NFH dramatic collapse caused by cooperative interactions
Characteristic reflectivity spectra should serve to validate our results experimentally
We have derived a SCFT considering the coupling of polymer elasticity, Flory-Huggins interactions, electrostatics, and local incompressibility. Using this theory, we have concluded the following:

## Slide 21: Outline
Future Work
SCFT Build-up
Systematic Study (Solubility vs. Internal Charge)
  Internal Structure of xC
Experimental Characterization (Reflectivity)
Experimental Application (Neurofilament-Heavy)
  Cooperative Collapse of the Dilute Layer

## Slide 22: Future Work
xC extension:
  Response to foreign species (e.g. spherical tip of AFM)
  Response to brush-brush
  Multivalent ions (ion correlations)
Experimental Collaborations
  Validation with reflectivity
  NF(L/M/H) blends for study of biological neurofilaments
    Erika Ding, Prof. Sanjay Kumar
  Nafion aggregation using SCFT-generated force fields and MD
    Siddarth Rajupet, Prof. Clayton Radke
Much more specific; physics /interactions of each problem
Highlight difficult problem and not that it’s a collaboration
What is your planned contribution

## Slide 23: Acknowledgements
Prof. Rui Wang
Dr. Chao Duan
Wang Group
Dr. Chao Fang
Nikhil Agrawal
Luofu Liu

## Slide 24: Summary
Paste from above when finished

## Slide 25: SI: Table of Contents
References
Introduction
  Alexander-de Gennes Brush
  SFBox numerical problem
  Borisov, 2001 (1Cd—1C)
SCFT Build-up
  Block copolymer SCFT
  Gaussian Chain
  Particle-to-field Transform,
  Hubbard-Stratonovich Transformation
  Propagator, derivation (CHECK)
  Flowchart (Numerics)
NFH
  Phase transition
  1Cd, 2Cd
Reflectivity
  Various ’s

## Slide 26: References
Abnormal NF image: Yuan, A., Rao, M. V., Veeranna, & Nixon, R. A. (2012). Neurofilaments at a glance. Journal of Cell Science, 125(14), 3257–3263. https://doi.org/10.1242/jcs.104729
Height Profile Figure: Srinivasan, N., Bhagawati, M., Ananthanarayanan, B., & Kumar, S. (2014). Stimuli-sensitive intrinsically disordered protein brushes. Nature Communications, 5(1), 5145. https://doi.org/10.1038/ncomms6145
Alexander-de Gennes Brush: Rubinstein, M., & Colby, R. H. (2003). Polymer Physics, Oxford University Press. New York.
Lubricity Figure: Yu, J., Jackson, N. E., Xu, X., Morgenstern, Y., Kaufman, Y., Ruths, M., de Pablo, J. J., & Tirrell, M. (2018). Multivalent counterions diminish the lubricity of polyelectrolyte brushes. Science, 360(6396), 1434–1438. https://doi.org/10.1126/science.aar5877
XR Multilayer Figure: Xu, H., Penfold, J., Thomas, R. K., Petkov, J. T., Tucker, I., & Webster, J. P. R. (2013). The Formation of Surface Multilayers at the Air–Water Interface from Sodium Polyethylene Glycol Monoalkyl Ether Sulfate/AlCl 3 Solutions: The Role of the Size of the Polyethylene Oxide Group. Langmuir, 29(37), 11656–11666. https://doi.org/10.1021/la4030348
Anti-Biofouling Figure: Chen, W.-L., Cordero, R., Tran, H., & Ober, C. K. (2017). 50th Anniversary Perspective: Polymer Brushes: Novel Surfaces for Future Materials. Macromolecules, 50(11), 4089–4113. https://doi.org/10.1021/acs.macromol.7b00450
XR Layout Figure: Schreiber, F., & Gerlach, A. (n.d.). X-Ray and Neutron Reflectivity. Department of Chemistry - University of Oxford. www.physchem.ox.ac.uk/~fs
XR Spectra Figure: Reinhardt, M., Dzubiella, J., Trapp, M., Gutfreund, P., Kreuzer, M., Gröschel, A. H., Müller, A. H. E., Ballauff, M., & Steitz, R. (2013). Fine-Tuning the Structure of Stimuli-Responsive Polymer Films by Hydrostatic Pressure and Temperature. Macromolecules, 46(16), 6541–6547. https://doi.org/10.1021/ma400962p

## Slide 27: Alexander-de Gennes Brush
Rubinstein, M., & Colby, R. H. (2003). Chapter 5.3
“Correlation length”
Monomers in correlation blobs (self-avoiding walk)
Height = Correlation length x No. Correlation blobs

## Slide 28: Borisov previous theory
Klushin, Birshtein, Amoskov. (2001). Macromolecules, 34.

## Slide 29: SFBox Lattice Artifacts
Pryamitsyn, V. A., Leermakers, F. A. M., Fleer, G. J., & Zhulina, E. B. (1996). Macromolecules, 29(25), 8260–8270.

## Slide 30: Block copolymer Free Energy, SCF Eqns
Variational Free Energy
  After statistical average over grafting surface (x-y plane)
Functional Minimization
SCF Equations

## Slide 31: Block copolymer PDEs
  Mean-field Poisson-Boltzmann Equation
  Modified Diffusion Equation
Block K
Block 2
Block 1

## Slide 32: SCFT Build-up — Flowchart
PDE Solve (for iteration k)
Propagate (using PDE solutions)
Check (for self-consistency)
Update (if not satisfied)
Anderson Mixing
Simple Mixing
Notation slightly incorrect but changed for clarity. w^{k} = f(w^{k+1/2}, w^{k-1}), where w^{k+1/2} is from SCFT calculations (\phi remains ^{k})

## Slide 33: Gaussian Chain
Large N, kb << 1
Generalize to whole chain with free internal segments
Probability of R with N
Bond vector distribution
Local Fluctuation
Configurational integral with free ends

## Slide 34: Particle-to-Field Transform

## Slide 35: Particle-to-Field Transform (2)
Cancels out

## Slide 36: Hubbard-Stratonovich Transformation
Constant, ignored
Electrolyte GCE

## Slide 37: Propagator notation

## Slide 38: Varying VdW () at const. Electrostatic ()
System:
Polymer distribution
Polymer smeared charge
Flory-Huggins parameter
Free energy

## Slide 39: Reflectivity — Different ’s

## Slide 40: NFH Phase Transition

## Slide 41: NFH 1Cd, 2Cd