## Slide 1: Microphase Segregation of Polyelectrolyte Brushes
Takashi Yokokura
Advisor: Prof. Rui Wang
UC Berkeley, Chemical and Biomolecular Engineering
Charged and Ion-Containing Polymers I
3/6/2023, 8:00 am - 11:00 am

## Slide 2: Introduction
Polyelectrolyte brushes (PEBs) are particularly promising for interfacial modification, “smart” materials, and as model systems in biology
(Chen, et al., Macromolecules, 2017 )
Biofouling
pH-sensitive flow valves
Lubrication
(Yuan, et. al., J. Cell Sci., 2012)
Aggregation mechanisms
Protein distribution
Mutation effects
A comprehensive understanding of the underlying physics is necessary for
  Discovery of new conformational targets and transition mechanisms
  Polymer design strategies for desired phenomena

## Slide 3: Motivation
Theory allows for the study of mechanisms and structures throughout the entire parameter space (chain length, charge fraction, solubility, etc.)
There has not been a systematic study of the coupling between polymer conformation and the interactions with its surroundings in PEBs
Standard buildup from statistical mechanics allows for straightforward implementation of additional interactions, such as
  Ion fluctuations (multivalent ions / charge inversion)
  Excluded volume effects
  Multi-chain interactions

## Slide 4: Presentation Overview
Theory
Systematic Study
Application to Experiments
Repulsive
Attractive

## Slide 5: Partition Function Formulation
Elastic entropy following Gaussian statistics
Flory-Huggins short-range interactions
Electrostatic correlations
Local incompressibility
+
-
+
-
+
-
+
+
+
-
-
-
+
s
s
s
s
s
s
s
s
s
s
s
+
+
+
+
+
+
+
+
+

## Slide 6: Free Energy and SCF Equations
Polymer Density:
Solvent Density:
Incompressibility:
Polymer-controlling Field:
Solvent-controlling Field:
Monomer Probability:
Electrostatic Potential:
Free Energy (ensemble average across surface)
Functional Minimization

## Slide 7: Presentation Overview
Theory
Systematic Study
Application to Experiments
Repulsive
Attractive

## Slide 8: Number of layers tunable with polymer charge fraction
High repulsion enriches conformational space
At intermediate repulsion, multiple condensed layers coexist with a dilute layer
High relative attraction eventually causes loss of sensitivity to repulsion
Key observations:
+
+
+
+
+
+
+
+
+
+
Repulsive
Attractive
s
s
s
s
s
s
s
s
s
s
s
s
For (const. repulsive)
Vol. fraction
Smeared charge
Flory-Huggins

## Slide 9: Chain organization within brush is deducible by SCFT
(Endpoint densities x 30)
“Locked-in-layer”
“Pearl-necklace-like”
Two candidates with identical averaged density profiles
4 condensed + 1 dilute
2 condensed
“Locked-in-layer” minimizes elastic penalty with mushroom conformations
Energetic cost of segregation scales with the “stem” traversing layers

## Slide 10: Presentation Overview
Theory
Systematic Study
Application to Experiments
Repulsive
Attractive

## Slide 11: Framework provides structural and mechanistic information for an IDP-derived brush
Coarse-graining
Neurofilament Heavy (NFH) chain
Experimental Comparison
Beyond Experiments
I
I

## Slide 12: Conclusions
SCFT accurately describes the coupled interactions within PEBs and provides experimentally inaccessible information
High charge fraction facilitates microphase segregation in PEBs
  Each layer as subsequent mushroom conformations (“locked-in-layer” model)
IDP brush derived from NFH is well-described by our model
  Polymer density profiles
  Predicted characterization spectra
    Reflectivity and brush-brush force

## Slide 13: Acknowledgements
Wang Group
  Prof. Rui Wang
  Dr. Chao Duan
  Nikhil Agrawal
  Luofu Liu
  Dr. Chao Fang
  Ian Woolsey
This material is based upon work supported by the National Science Foundation Graduate Research Fellowship under Grant No. DGE 2146752

## Slide 14: Thank you!
Systematic Study
Application to IDP

## Slide 15: Supplemental Slides
Full partition function
NFH pressure dilute-coex transition mechanism
NFH coarse-graining parameters (and H formula)
Henderson-Hasselbalch
SCFT Flowchart
Reflectivity master equation
Block-polymer SCFT equations

## Slide 16: Full Partition Function
Elastic entropy following Gaussian statistics
Flory-Huggins short-range interactions
Electrostatic correlations
Local incompressibility
Semicanonical Ensemble
(Indices) : Solvent; : Cation; : Anion
(Subscripts) : Solvent; : Polymer; : Charged
Particle Operators
Coulomb Operator

## Slide 17: NFH pressure dilute-coex transition
4 mM vs. 6 mM mechanisms

## Slide 18: NFH Coarse-graining parameters
Vol. frac to height
Kuhn’s length and monomer volume:
b = 3.00 nm
v = 1.30 nm3

## Slide 19: Henderson-Hasselbalch
AA | pKa | pKb
D (Aspartic Acid) | 3.65 | 
E (Glutamic Acid) | 4.25 | 
K (Lysine) |  | 10.53
R (Arginine) |  | 12.48
H (Histidine) |  | 6.00

## Slide 20: SCFT Build-up — Flowchart
PDE Solve (for iteration k)
Propagate (using PDE solutions)
Check (for self-consistency)
Update (if not satisfied)
Anderson Mixing
Simple Mixing
Notation slightly incorrect but changed for clarity. w^{k} = f(w^{k+1/2}, w^{k-1}), where w^{k+1/2} is from SCFT calculations (\phi remains ^{k})

## Slide 21: Reflectivity Master Equation Derivation
Russel, T.P., Materials Science Reports, 1990
“missing” length dimension
C =i ; from integration over all area elements at z
Phase factor for interference:
Integration by parts
Qz notation, non-normalized density, Fresnel reflectivity
Continuous density profile (Reimann sum analogue)
Scattered amplitude
Incident amplitude
Wavelength
Scattering density proflile
Incident angle
2
Scattering vector

## Slide 22: Block copolymer PDEs
  Mean-field Poisson-Boltzmann Equation
  Modified Diffusion Equation
Block K
Block 2
Block 1