## Slide 1: Structural and Mechanical Properties of Polyelectrolyte Brushes
Takashi Yokokura
Advisor: Prof. Rui Wang
September 14th, 10:00 am – 12:00 pm
Qualifying Exam

## Slide 2: Introduction
Polymer Brush
  Chains end-fixed to some substrate
  Steric interactions extend chains into solution
Conformational possibilities
  Coexistence between dilute, coil-like layer and condensed layer
Polyelectrolyte Brush
  Monomers contain charge
  Long-range electrostatic interactions drive extension
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
Model system for biological aggregates
  Axon stabilization through neurofilaments
Designable functionalized surface
  Anti-fouling
  “Smart” sensors
Cell-repellant Surface
(Yuan, et. al., J. Cell Sci., 2012)
(Chen, et al., Macromolecules, 2017 )

## Slide 3: Previous Theories
Flory scaling – de Gennes, Alexander
Drawbacks:
  Elasticity is inaccurately considered
  Effects from multivalent ions cannot be aptured
Correlation length:
No. monomers in correlation blob:
Brush height:
Lattice-constrained Scheutjens-Fleer SCFT
(Rubinstein, Colby, Oxford Univ. Press, 2003)
(Yu et al., Science, 2018)
6 mM Na+
0.01 mM Ca2+
0.1 mM Ca2+
1 mM Ca2+
1 mM Ba2+
Kuhn monomer length
Read more

## Slide 4: Presentation Overview
Theory
Systematic Study
Application to Experiments
Brush Response to Ionic Strength
Repulsive
Attractive

## Slide 5: Outline
Model and Theory Development
Particle description
111
Field description
111
Self-consistent field theory

## Slide 6: Model and Theory Development — System
Interactions:
Elasticity (monomer-monomer)
Solubility (solvent-monomer)
Electrostatics (ion-monomer)
+
-
+
-
+
-
+
+
+
-
-
-
+
s
s
s
s
s
s
s
s
s
s
s
+
+
+
+
+
+
+
+
+
What is the system made up of?
Polymer curve
Discrete particle locations

## Slide 7: Model and Theory Development— Interactions
Elastic entropy following Gaussian statistics
Flory-Huggins short-range interactions
Electrostatic correlations over Coulomb operator
Local incompressibility
Semicanonical Ensemble

## Slide 8: Model and Theory Development— Interactions
Particle-to-Field Transformation
111
Saddle-point approximation
Hubbard-Stratonovich Transformation
111

## Slide 9: Model and Theory Development — SCF Eqns
Polymer Density:
Solvent Density:
Incompressibility:
Polymer-controlling Field:
Solvent-controlling Field:
Monomer Probability:
Electrostatic Potential:
Free Energy (ensemble average across surface)
Functional Minimization

## Slide 10: Outline
Systematic Study (VdW Attraction vs. Electrostatic Repulsion)
+
+
+
+
+
+
+
+
+
+
Repulsive
Attractive
s
s
s
s
s
s
s
s
s
s
s
s
Polymer charge fraction
(Electrostatic repulsion)
Hydrophobicity
(VdW attraction)

## Slide 11: Varying VdW () at const. Electrostatic ()
Height
0
(nm)
System:
Polymer distribution
Polymer smeared charge
Flory-Huggins parameter
Free energy
1 condensed layer
2 condensed layers
0
0
C = “condensed” layer(s)
Polymer density profiles
1 condensed layer
2 condensed layers
3 condensed layers
4 condensed layers + 1 dilute layer
Similar “multi-layered” structures in dilute polyelectrolyte solutions
Repulsion promotes segregation, while hydrophobicity and elasticity promote condensation
Not predicted before for brushes
(Duan and Wang, JCP, 2020)

## Slide 12: Varying VdW and Smeared Charge Fraction
System:
Polymer distribution
Polymer smeared charge
Flory-Huggins parameter
Higher polymer charge leads to richer conformational space
Coexistence with dilute layer adjacent to the dilute regime
As attraction becomes dominant, brushes insensitive to charge
Attraction
Repulsion
(nm)
C = “condensed” layer(s)
d Criteria of phi_p = 0.5

## Slide 13: Chain Architecture of Multi-peaked Conformations
(Endpoint densities x 30)
“Locked-in-layer”
“Pearl-necklace-like”
Two candidates with identical averaged density profiles
4 condensed + 1 dilute
Chains stay within one layer, regardless if condensed or dilute
2 condensed

## Slide 14: Outline
Reflectivity Spectra for Multi-peak conformations
Substrate
Sample
Incident radiation
Measured radiation

## Slide 15: Reflectivity
Reflectivity provides characterization of vertically stacked films (layers)
Specular wave scattering vector
(Schreiber, n.d.)
(Reinhardt, et. al. Macromolecules, 2013)
Polymer profiles are guessed
SCFT-generated Reflectivity Spectra

## Slide 16: Outline
Application of Theory to Neurofilament-Heavy (NFH) Protein Brush
(Srinivasan, 2014)
(Yuan, 2012)
“Heavy”
“… AQGEEEEEAEEGGEEAATTSPPA …”

## Slide 17: Coarse Graining NFH at pH 2.4
Cusum
Cusum slope
Coarse-grained charge distribution

## Slide 18: Cooperative Collapse of the Dilute Phase
What changes are occurring within NFH during 3x decrease?
Dramatic collapse
2Cd
2C
1C
“Cooperative collapse”
Chain collapse from screening facilitates further collapse by lowering effective grafting density
Comparison with Experimental Results

## Slide 19: Summary
Multi-peaked conformations are caused by the balance of
Electrostatics (repulsion)
Hydrophobicity and elasticity (attraction)
Each chain is allowed in only one layer. Outer layers are “grafted” upon inner layers.
Cooperative interactions in NFH between ionic strength and effective grafting density causes a 3x decrease in height.
SCFT-generated reflectivity spectra should facilitate experimental evidence of multi-peaked conformations
We have derived an SCFT considering the coupling of polymer elasticity, Flory-Huggins interactions, electrostatics, and local incompressibility. Using this theory, we have concluded the following:

## Slide 20: Future Work
xC extension:
  Response to foreign species (e.g. spherical tip of AFM)
  Response to brush-brush
  Multivalent ions (ion correlations)
Much more specific; physics /interactions of each problem

## Slide 21: Future Work
Experimental Collaborations
  Validation with reflectivity
  NF(L/M/H) blends for study of biological neurofilaments
    Erika Ding, Prof. Sanjay Kumar
  Nafion aggregation using SCFT-generated force fields and MD
    Siddarth Rajupet, Prof. Clayton Radke
What is your planned contribution
Highlight difficult problem and not that it’s a collaboration

## Slide 22: Acknowledgements
Prof. Rui Wang
Dr. Chao Duan
Wang Group
Dr. Chao Fang
Nikhil Agrawal
Luofu Liu

## Slide 23: Summary
Paste from above when finished

## Slide 24: SI: Table of Contents
References
Introduction
  Alexander-de Gennes Brush
  Surface Force Apparatus
  SFBox numerical problem
  Borisov, 2001 (1Cd—1C)
SCFT Build-up
  Block copolymer SCFT
  Gaussian Chain
  Particle-to-field Transform,
  Hubbard-Stratonovich Transformation
  Propagator, derivation (CHECK)
  Flowchart (Numerics)
NFH
  Phase transition
  1Cd, 2Cd
Reflectivity
  Various ’s
Presentation Outlines:
Title
Model and Theory
Systematic Study
Reflectivity
NFH
Summary
Future Work

## Slide 25: References
Abnormal NF image: Yuan, A., Rao, M. V., Veeranna, & Nixon, R. A. (2012). Neurofilaments at a glance. Journal of Cell Science, 125(14), 3257–3263. https://doi.org/10.1242/jcs.104729
Height Profile Figure: Srinivasan, N., Bhagawati, M., Ananthanarayanan, B., & Kumar, S. (2014). Stimuli-sensitive intrinsically disordered protein brushes. Nature Communications, 5(1), 5145. https://doi.org/10.1038/ncomms6145
Alexander-de Gennes Brush: Rubinstein, M., & Colby, R. H. (2003). Polymer Physics, Oxford University Press. New York.
Lubricity Figure: Yu, J., Jackson, N. E., Xu, X., Morgenstern, Y., Kaufman, Y., Ruths, M., de Pablo, J. J., & Tirrell, M. (2018). Multivalent counterions diminish the lubricity of polyelectrolyte brushes. Science, 360(6396), 1434–1438. https://doi.org/10.1126/science.aar5877
XR Multilayer Figure: Xu, H., Penfold, J., Thomas, R. K., Petkov, J. T., Tucker, I., & Webster, J. P. R. (2013). The Formation of Surface Multilayers at the Air–Water Interface from Sodium Polyethylene Glycol Monoalkyl Ether Sulfate/AlCl 3 Solutions: The Role of the Size of the Polyethylene Oxide Group. Langmuir, 29(37), 11656–11666. https://doi.org/10.1021/la4030348
Anti-Biofouling Figure: Chen, W.-L., Cordero, R., Tran, H., & Ober, C. K. (2017). 50th Anniversary Perspective: Polymer Brushes: Novel Surfaces for Future Materials. Macromolecules, 50(11), 4089–4113. https://doi.org/10.1021/acs.macromol.7b00450
XR Layout Figure: Schreiber, F., & Gerlach, A. (n.d.). X-Ray and Neutron Reflectivity. Department of Chemistry - University of Oxford. www.physchem.ox.ac.uk/~fs
XR Spectra Figure: Reinhardt, M., Dzubiella, J., Trapp, M., Gutfreund, P., Kreuzer, M., Gröschel, A. H., Müller, A. H. E., Ballauff, M., & Steitz, R. (2013). Fine-Tuning the Structure of Stimuli-Responsive Polymer Films by Hydrostatic Pressure and Temperature. Macromolecules, 46(16), 6541–6547. https://doi.org/10.1021/ma400962p

## Slide 26: Alexander-de Gennes Brush
Rubinstein, M., & Colby, R. H. (2003). Chapter 5.3
“Correlation length”
Monomers in correlation blobs (self-avoiding walk)
Height = Correlation length x No. Correlation blobs

## Slide 27: Surface Force Apparatus (SFA)
Distance (D) is calculated using a spectrometer, which generates Fringes of Equal Chromatic Order (FECO)
  Mirrors allow only wavelengths that form standing waves between to constructively interfere
  Distance is measured by relating FECO wavelength to that from mica in contact
Lowrey, D. D., Tasaka, K., Kindt, J. H., Banquy, X., Belman, N., Min, Y., Pesika, N. S., Mordukhovich, G., & Israelachvili, J. N. (2011). High-Speed Friction Measurements Using a Modified Surface Forces Apparatus. Tribology Letters, 42(1), 117–127. https://doi.org/10.1007/s11249-011-9746-1

## Slide 28: Borisov previous theory
Klushin, Birshtein, Amoskov. (2001). Macromolecules, 34.

## Slide 29: SFBox Lattice Artifacts
Pryamitsyn, V. A., Leermakers, F. A. M., Fleer, G. J., & Zhulina, E. B. (1996). Macromolecules, 29(25), 8260–8270.

## Slide 30: Block copolymer Free Energy, SCF Eqns
Variational Free Energy
  After statistical average over grafting surface (x-y plane)
Functional Minimization
SCF Equations

## Slide 31: Block copolymer PDEs
  Mean-field Poisson-Boltzmann Equation
  Modified Diffusion Equation
Block K
Block 2
Block 1

## Slide 32: SCFT Build-up — Flowchart
PDE Solve (for iteration k)
Propagate (using PDE solutions)
Check (for self-consistency)
Update (if not satisfied)
Anderson Mixing
Simple Mixing
Notation slightly incorrect but changed for clarity. w^{k} = f(w^{k+1/2}, w^{k-1}), where w^{k+1/2} is from SCFT calculations (\phi remains ^{k})

## Slide 33: Gaussian Chain
Large N, kb << 1
Generalize to whole chain with free internal segments
Probability of R with N
Bond vector distribution
Local Fluctuation
Configurational integral with free ends

## Slide 34: Particle-to-Field Transform

## Slide 35: Particle-to-Field Transform (2)
Cancels out

## Slide 36: Hubbard-Stratonovich Transformation
Constant, ignored
Electrolyte GCE

## Slide 37: Propagator notation

## Slide 38: Varying VdW () at const. Electrostatic ()
System:
Polymer distribution
Polymer smeared charge
Flory-Huggins parameter
Free energy

## Slide 39: Reflectivity — Different ’s

## Slide 40: NFH Phase Transition

## Slide 41: NFH 1Cd, 2Cd