## Slide 1: Structural and Mechanical Properties of Polyelectrolyte Brushes
Takashi Yokokura
Advisor: Prof. Rui Wang
September 14th, 10:00 am – 12:00 pm
Qualifying Exam

## Slide 2: Introduction
Polymer Brush
  Chains end-fixed to some substrate
  Steric interactions extend chains into solution
Conformational possibilities
  Coexistence between dilute, coil-like layer and condensed layer
Polyelectrolyte Brush
  Monomers contain charge
  Long-range electrostatic interactions drive extension
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
Model system for biological aggregates
  Axon stabilization through neurofilaments
Designable functionalized surface
  Anti-fouling
  “Smart” sensors
Cell-repellant Surface
(Yuan, et. al., J. Cell Sci., 2012)
(Chen, et al., Macromolecules, 2017 )

## Slide 3: Previous Theories
Flory scaling – de Gennes, Alexander
Drawbacks:
  Elasticity is inaccurately considered
  Effects from multivalent ions cannot be captured
Correlation length:
No. monomers in correlation blob:
Brush height:
Lattice-constrained Scheutjens-Fleer SCFT
(Rubinstein, Colby, Oxford Univ. Press, 2003)
(Yu et al., Science, 2018)
6 mM Na+
0.01 mM Ca2+
0.1 mM Ca2+
1 mM Ca2+
1 mM Ba2+
Kuhn monomer length
Scaling exponent, 0.588

## Slide 4: Presentation Overview
Theory
Systematic Study
Application to Experiments
Brush Response to Ionic Strength
Repulsive
Attractive

## Slide 5: Outline
Model and Theory Development
Particle description
111
Field description
111
Self-consistent field theory

## Slide 6: System Species and Interactions
Interactions:
Elasticity (monomer-monomer)
Solubility (solvent-monomer)
Electrostatics (ion-monomer)
+
-
+
-
+
-
+
+
+
-
-
-
+
s
s
s
s
s
s
s
s
s
s
s
+
+
+
+
+
+
+
+
+
What is the system made up of?
Polymer curve
Discrete particle locations
(Indices) : Solvent; : Cation; : Anion

## Slide 7: Partition Function Formulation
Elastic entropy following Gaussian statistics
Flory-Huggins short-range interactions
Electrostatic correlations
Local incompressibility
Semicanonical Ensemble
(Indices) : Solvent; : Cation; : Anion
(Subscripts) : Solvent; : Polymer; : Charged
Particle Operators
Coulomb Operator

## Slide 8: Partition Function Simplification
Particle-to-Field Transformation
111
Saddle-point approximation
Hubbard-Stratonovich Transformation
111
Particle Operators
Coulomb Operator

## Slide 9: Free Energy and SCF Equations
Polymer Density:
Solvent Density:
Incompressibility:
Polymer-controlling Field:
Solvent-controlling Field:
Monomer Probability:
Electrostatic Potential:
Free Energy (ensemble average across surface)
Functional Minimization

## Slide 10: Outline
Systematic Study (VdW Attraction vs. Electrostatic Repulsion)
+
+
+
+
+
+
+
+
+
+
Repulsive
Attractive
s
s
s
s
s
s
s
s
s
s
s
s
Polymer charge fraction
(Electrostatic repulsion)
Hydrophobicity
(VdW attraction)

## Slide 11: Multi-layered conformations arise at high relative repulsion
Height
0
(nm)
System:
Polymer distribution
Polymer smeared charge
Flory-Huggins parameter
Free energy
1 condensed layer
2 condensed layers
0
0
C = “condensed” layer(s)
Polymer density profiles
1 condensed layer
2 condensed layers
3 condensed layers
4 condensed layers + 1 dilute layer
Similar “multi-layered” structures in dilute polyelectrolyte solutions
Repulsion promotes segregation, while hydrophobicity and elasticity promote condensation
Not predicted before for brushes
(Duan and Wang, JCP, 2020)
Constant polymer charge fraction ()

## Slide 12: Number of layers tunable with polymer charge fraction
System:
Polymer distribution
Polymer smeared charge
Flory-Huggins parameter
Attraction
Repulsion
(nm)
C = “condensed” layer(s)
High repulsion enriches conformational space
At intermediate repulsion, multiple condensed layers coexist with a dilute layer
High relative attraction eventually causes loss of sensitivity to repulsion
Key observations:

## Slide 13: Chain organization within brush is deducible by SCFT
(Endpoint densities x 30)
“Locked-in-layer”
“Pearl-necklace-like”
Two candidates with identical averaged density profiles
4 condensed + 1 dilute
2 condensed
“Locked-in-layer” minimizes elastic penalty using mushroom conformations
Energetic cost of segregation scales with number of monomers within the “stem” traversing layers

## Slide 14: Outline
Reflectivity Spectra for Multi-peak conformations
Substrate
Sample
Incident radiation
Measured radiation

## Slide 15: Multi-layer conformations generate highly convoluted reflectivity spectra
Reflectivity provides characterization of vertically stacked films (layers)
Specular wave scattering vector
(Schreiber, n.d.)
(Reinhardt, et. al. Macromolecules, 2013)
Polymer profiles are guessed
SCFT-generated Reflectivity Spectra
Highly convoluted spectra caused by different layer interfaces within multi-layer brushes
Fitting such spectra requires a model that can accurately capture coupled interactions, especially elastic

## Slide 16: Outline
Application of Theory to Neurofilament-Heavy (NFH) Protein Brush
(Srinivasan, 2014)
(Yuan, 2012)
“Heavy”
Block K
Block 2
Block 1
“… AQGEEEEEAEEGGEEAATTSPPA …”
Coarse-grained mapping

## Slide 17: Cusum-generated bins effectively coarse-grain NFH charge distribution
Cusum
Cusum slope
Coarse-grained charge distribution
“… AQGEEEEEAEEGGEEAATTSPPA …”

## Slide 18: Dramatic collapse caused by cooperative collapse of dilute layer
What changes are occurring within NFH during 3x decrease?
Dramatic collapse
2Cd
2C
1C
“Cooperative collapse”
Comparison with Experimental Results
Sensitivity of stimuli-sensitive brush is dependent on internal chain organization and cooperative collapse unique to dilute layer

## Slide 19: Summary
Multi-layered conformations are caused by the balance of
Electrostatics (repulsion)
Hydrophobicity and elasticity (attraction)
Chains stay within one layer to minimize overall elastic penalty
Subsequent layers are “grafted upon” previous layers
The dramatic collapse of the NFH brush is due to cooperative effects specific to a dilute layer coexisting with condensed layers
SCFT-generated reflectivity spectra should facilitate experimental evidence of multi-peaked conformations
We have derived an SCFT considering the coupling of polymer elasticity, Flory-Huggins interactions, electrostatics, and local incompressibility. Using this theory, we have concluded the following:

## Slide 20: Future Work — Considering electrostatic fluctuations through the ion self energy
Multivalent ions facilitate multi-layer brushes at low ionic concentrations and bridging effects between opposing brushes
  No current theories can capture either phenomena
(Yu et al., Science, 2018; Xu et al., Langmuir, 2013; Wang Phys Rev E, 2010)
6 mM Na+
0.01 mM Ca2+
0.1 mM Ca2+
1 mM Ca2+
1 mM Ba2+
AlCl3 Concentration [mM]
SLE3S Concentration [mM]
Next project will study the attractive force between interacting brushes in multivalent solutions
  Equations need to include ion fluctuations
  Computational efficiency for solving Green’s function
Permittivity
The “modified PB equation” contains ion self energy, which describes the energy of charge fluctuations
Ion fluctuations are needed to consider inhomogeneous dielectric media and specific ion effects
Ion distribution:
Ion radius
Ion self energy

## Slide 21: Future Work — Effect of mixture compositions and sidearm sequences on neurofilaments
Theory is modified to consider mixtures of L/M/H
  As for NFH results, SCFT provides experimentally inaccessible polymer profiles and structure
  Future contributions include ternary phase diagrams and the role of sequences on overall neurofilament structure and response
Light (L)
Medium (M)
Heavy (H)
pH = 7.44
Length [nm]
Polymer Density
Black: Overall
Red: L
Purple: M
Blue: H
Neurofilaments are mainly composed of 3 chain types (L/M/H), whose composition is strictly regulated during development
  Sidearms have evolved into considerably different sequences

## Slide 22: Acknowledgements
Prof. Rui Wang
Dr. Chao Duan
Wang Group
Dr. Chao Fang
Nikhil Agrawal
Luofu Liu

## Slide 23: Summary
Multi-layered conformations are caused by the balance of
Electrostatics (repulsion)
Hydrophobicity and elasticity (attraction)
Chains stay within one layer to minimize overall elastic penalty
Subsequent layers are “grafted upon” previous layers
The dramatic collapse of the NFH brush is due to cooperative effects specific to a dilute layer coexisting with condensed layers
SCFT-generated reflectivity spectra should facilitate experimental evidence of multi-peaked conformations
We have derived an SCFT considering the coupling of polymer elasticity, Flory-Huggins interactions, electrostatics, and local incompressibility. Using this theory, we have concluded the following:

## Slide 24: SI: Table of Contents
References
Introduction
  Alexander-de Gennes Brush
  Surface Force Apparatus
  SFBox numerical problem
  Borisov, 2001 (1Cd—1C)
SCFT Build-up
  Block copolymer SCFT
  Gaussian Chain
  Particle-to-field Transform,
  Hubbard-Stratonovich Transformation
  Propagator, derivation
  Flowchart (Numerics)
a040 video
NFH
  Phase transition
  1Cd, 2Cd
Reflectivity
  Various ’s
Presentation Outlines:
Title
Model and Theory
Systematic Study
Reflectivity
NFH
Summary
Future Work

## Slide 25: References
Abnormal NF image: Yuan, A., Rao, M. V., Veeranna, & Nixon, R. A. (2012). Neurofilaments at a glance. Journal of Cell Science, 125(14), 3257–3263. https://doi.org/10.1242/jcs.104729
Height Profile Figure: Srinivasan, N., Bhagawati, M., Ananthanarayanan, B., & Kumar, S. (2014). Stimuli-sensitive intrinsically disordered protein brushes. Nature Communications, 5(1), 5145. https://doi.org/10.1038/ncomms6145
Alexander-de Gennes Brush: Rubinstein, M., & Colby, R. H. (2003). Polymer Physics, Oxford University Press. New York.
Lubricity Figure: Yu, J., Jackson, N. E., Xu, X., Morgenstern, Y., Kaufman, Y., Ruths, M., de Pablo, J. J., & Tirrell, M. (2018). Multivalent counterions diminish the lubricity of polyelectrolyte brushes. Science, 360(6396), 1434–1438. https://doi.org/10.1126/science.aar5877
XR Multilayer Figure: Xu, H., Penfold, J., Thomas, R. K., Petkov, J. T., Tucker, I., & Webster, J. P. R. (2013). The Formation of Surface Multilayers at the Air–Water Interface from Sodium Polyethylene Glycol Monoalkyl Ether Sulfate/AlCl 3 Solutions: The Role of the Size of the Polyethylene Oxide Group. Langmuir, 29(37), 11656–11666. https://doi.org/10.1021/la4030348
Anti-Biofouling Figure: Chen, W.-L., Cordero, R., Tran, H., & Ober, C. K. (2017). 50th Anniversary Perspective: Polymer Brushes: Novel Surfaces for Future Materials. Macromolecules, 50(11), 4089–4113. https://doi.org/10.1021/acs.macromol.7b00450
XR Layout Figure: Schreiber, F., & Gerlach, A. (n.d.). X-Ray and Neutron Reflectivity. Department of Chemistry - University of Oxford. www.physchem.ox.ac.uk/~fs
XR Spectra Figure: Reinhardt, M., Dzubiella, J., Trapp, M., Gutfreund, P., Kreuzer, M., Gröschel, A. H., Müller, A. H. E., Ballauff, M., & Steitz, R. (2013). Fine-Tuning the Structure of Stimuli-Responsive Polymer Films by Hydrostatic Pressure and Temperature. Macromolecules, 46(16), 6541–6547. https://doi.org/10.1021/ma400962p

## Slide 26: Alexander-de Gennes Brush
Rubinstein, M., & Colby, R. H. (2003). Chapter 5.3
“Correlation length”
Monomers in correlation blobs (self-avoiding walk)
Height = Correlation length x No. Correlation blobs

## Slide 27: Surface Force Apparatus (SFA)
Distance (D) is calculated using a spectrometer, which generates Fringes of Equal Chromatic Order (FECO)
  Mirrors allow only wavelengths that form standing waves between to constructively interfere
  Distance is measured by relating FECO wavelength to that from mica in contact
Lowrey, D. D., Tasaka, K., Kindt, J. H., Banquy, X., Belman, N., Min, Y., Pesika, N. S., Mordukhovich, G., & Israelachvili, J. N. (2011). High-Speed Friction Measurements Using a Modified Surface Forces Apparatus. Tribology Letters, 42(1), 117–127. https://doi.org/10.1007/s11249-011-9746-1

## Slide 28: SFBox Lattice Artifacts
Pryamitsyn, V. A., Leermakers, F. A. M., Fleer, G. J., & Zhulina, E. B. (1996). Macromolecules, 29(25), 8260–8270.

## Slide 29: Borisov previous theory
Klushin, Birshtein, Amoskov. (2001). Macromolecules, 34.

## Slide 30: Block copolymer Free Energy, SCF Eqns
Variational Free Energy
  After statistical average over grafting surface (x-y plane)
Functional Minimization
SCF Equations

## Slide 31: Block copolymer PDEs
  Mean-field Poisson-Boltzmann Equation
  Modified Diffusion Equation
Block K
Block 2
Block 1

## Slide 32: SCFT Build-up — Flowchart
PDE Solve (for iteration k)
Propagate (using PDE solutions)
Check (for self-consistency)
Update (if not satisfied)
Anderson Mixing
Simple Mixing
Notation slightly incorrect but changed for clarity. w^{k} = f(w^{k+1/2}, w^{k-1}), where w^{k+1/2} is from SCFT calculations (\phi remains ^{k})

## Slide 33: Gaussian Chain
Large N, kb << 1
Generalize to whole chain with free internal segments
Probability of R with N
Bond vector distribution
Local Fluctuation
Configurational integral with free ends

## Slide 34: Particle-to-Field Transform

## Slide 35: Particle-to-Field Transform (2) & Qs, Qp
Cancels out

## Slide 36: Hubbard-Stratonovich Transformation
Constant, ignored
Electrolyte GCE

## Slide 37: Propagator notation
“Chain energy” between s1 and s2 in curve R
“Propagator” from Boltzmann factor and known endpoints of chain end (0) and contour length s
Forward propagator

## Slide 38: MDE Derivation

## Slide 39: Varying VdW () at const. Electrostatic ()
System:
Polymer distribution
Polymer smeared charge
Flory-Huggins parameter
Free energy

## Slide 40: Reflectivity Master Equation Derivation
Russel, T.P., Materials Science Reports, 1990
“missing” length dimension
C =i ; from integration over all area elements at z
Phase factor for interference:
Integration by parts
Qz notation, non-normalized density, Fresnel reflectivity
Continuous density profile (Reimann sum analogue)
Scattered amplitude
Incident amplitude
Wavelength
Scattering density proflile
Incident angle
2
Scattering vector

## Slide 41: Reflectivity — Different ’s

## Slide 42: Henderson-Hasselbalch
AA | pKa | pKb
D (Aspartic Acid) | 3.65 | 
E (Glutamic Acid) | 4.25 | 
K (Lysine) |  | 10.53
R (Arginine) |  | 12.48
H (Histidine) |  | 6.00

## Slide 43: NFH Phase Transition

## Slide 44: NFH 1Cd, 2Cd

## Slide 45: Self energy
Fluctuating field
Ion charge distribution:
Reference action:
Ion radius
Average (saddle-point) field
Ion self energy
Gibbs-Feynman-Bogoliubov Inequality:
After Hubbard-Stratonovich
Grand Free Energy:
Minimization wrt
ref